## Slide 1: Introduction to Catalysis
William F. Schneider

## Slide 2: What is a “Catalyst”
A catalyst (Greek: καταλύτης, catalytēs) is a substance that accelerates the rate of a chemical reaction without itself being transformed or consumed by the reaction. (Wikipedia)
A + B
C
ΔG
Ea
uncatalyzed
A + B +
catalyst
C + catalyst
ΔG
Ea′
catalyzed
k(T) = k0e-Ea/RT
Ea′ < Ea
k0′ > k0
k′ > k
ΔG = ΔG

## Slide 3: Catalysts Open Up New Reaction Pathways
CH3
C
CH3
O
CH2
C
CH3
OH
propanone
propenol
H2C
H
O
C
CH3
‡
‡
propanone
propenol

## Slide 4: Catalysts Open Up New Reaction Pathways
CH3
C
CH3
O
CH2
C
CH3
OH
OH−
CH2
C
CH3
O−
+ H2O
−OH−
Base catalyzed
propanone
propenol
intermediate
‡
‡
rate = k[OH−][acetone]

## Slide 5: Catalysts Open Up New Reaction Pathways
CH3
C
CH3
O
CH2
C
CH3
OH
+ H2O
Acid catalyzed
H3O+
CH3
C
CH3
OH
+
−H3O+
propenol
different
intermediate
‡
‡
propanone
rate = k[H3O+][acetone]

## Slide 6: Types of Catalysts - Enzymes
The “Gold Standard” of catalysts
Highly specific
Highly selective
Highly efficient
Catalyze very difficult reactions
  N2  NH3
  CO2 + H2O  C6H12O6
Works better in a cell than in a 100000 l reactor
Triosephosphateisomerase
“TIM”
Cytochrome C Oxidase
Highly tailored “active sites”
Often contain metal atoms

## Slide 7: Types of Catalysts – Organometallics
Perhaps closest man has come to mimicking nature’s success
2005 Noble Prize in Chemistry
Well-defined, metal-based active sites
Selective, efficient manipulation of organic functional groups
Various forms, especially for polymerization catalysis
Difficult to generalize beyond organic transformations
ROMP:

## Slide 8: Homogeneous vs. Heterogeneous Catalysts
Homogeneous catalysis
Single phase
(Typically liquid)
Low temperature
Separations are tricky
Heterogeneous catalysis
Multiphase
(Mostly solid-liquid and solid-gas)
High temperature
Design and optimization tricky
Zeolite catalyst
Catalyst powders

## Slide 9: Microporous Catalysts
Porous on the scale of molecular dimensions
  10 – 100 Å
  Up to 1000’s m2/g surface area
Catalysis through
  shape selection
  acidity/basicity
  incorporation of metal particles
10 Å
100 Å
Zeolite (silica-aluminate)
MCM-41 (mesoporous silica)
Metal-organic framework
(2025 Nobel Prize)

## Slide 10: Amorphous Heterogeneous Catalysts
Amorphous, high surface area supports
  Alumina, silica, activated carbon, …
  Up to 100’s of m2/g of surface area
Impregnated with catalytic transition metals
  Pt, Pd, Ni, Fe, Ru, Cu, Ru, …
Typically pelletized or on monoliths
Cheap, high stability, catalyze many types of reactions
Most used, least well understood of all classes
SEM micrographs of alumina and Pt/alumina

## Slide 11: Sample Heterogeneous Catalytic Processes
Haber-Bosch process
  N2 + 3 H2 → 2 NH3
  Fe/Ru catalysts, high pressure and temperature
  Critical for fertilizer and nitric acid production
Fischer-Tropsch chemistry
  n CO + 2n H2 → (CH2)n + n H2O , syn gas to liquid fuels
  Fe/Co catalysts
  Source of fuel for Axis in WWII
Water-gas shift
  CO + H2O → CO2 + H2
  Pd catalysts
  Important in H2 production
Fluidized catalytic cracking
  High MW petroleum → low MW fuels, like gasoline
  Zeolite catalysts, high temperature combustor
  In your fuel tank!
Automotive three-way catalysis
  NOx/CO/HC → H2O/CO2/H2O
  Pt/Rh/Pd supported on ceria/alumina
  Makes exhaust 99% cleaner

## Slide 12: Heterogeneous Catalytic Reactors
Design goals
  rapid and intimate contact between catalyst and reactants
  ease of separation of products from catalyst
Slurry
Reactor
Fluidized
Bed
Catalyst
Recycle
Reactor
Packed
Bed

## Slide 13: Length Scales in Heterogeneous Catalysis
Mass transport/diffusion
Chemical adsorption and reaction

## Slide 14: Characteristics of Supported Catalysts
Surface area:
  Amount of internal support surface accessible to a fluid
  Measured by gas adsorption isotherms
Loading:
  Mass of transition metal per mass of support
Dispersion:
  Percent of metal atoms accessible to a fluid
support
M
M
M

## Slide 15: Transition Metal Catalysts
More inert
Filling d shell
More active
Harder to reduce
Easier to reduce
Metal particle exposing facets

## Slide 16: Adsorption and Reaction at Solid Surfaces
Physisorption: weak van der Waals attraction of a fluid (like N2 gas) for any surface
  Eads ~10 – 40 kJ/mol
  Low temperature phenomenon
  Exploited in measuring gross surface area
Chemisorption: chemical bond formation between a fluid molecule (like CO or ethylene) and a surface site
  Eads ~ 100 – 500 kJ/mol
  Essential element of catalytic activity
  Exploited in measuring catalytically active sites

## Slide 17: Physi- and Chemisorption on MgO(001)
CO2
SO2
Physisorbed CO2
-10 kJ mol-1 GGA
Chemisorbed SO2
(“sulfite”)
-100 kJ mol-1 GGA
SO3
Chemisorbed SO3
(“sulfate”)
-200 kJ mol-1 GGA
MgO(001) supercell
Mg
O
:
Schneider, Li, and Hass, J. Phys. Chem. B 2001, 105, 6972

## Slide 18: Concentrations in Heterogeneous Catalysis
Fluid concentrations
  Traditionally reported as pressures (torr, atm, bar)
  Ideal gas assumption: Pj = Cj RT
Surface concentrations
  “Coverage” per unit area
    nj = molesj / area
  Maximum coverage called monolayer
    1 ML: nj,max = ~ 1015 molecules / cm2
  Fractional coverage
    θj = nj / nj,max
    0 ≤ θj ≤ 1
θj = 1/6
Rate = f(Pj,θj)
Metal particle surface

## Slide 19: Adsorption Isotherms
Molecules in gas and surface are in dynamic equilibrium
A (g) + M (surface) ⇌ M-A
Isotherm describes pressure dependence of equilibrium
Langmuir isotherm proposed by Irving Langmuir, GE, 1915
  Adsorption saturates at 1 monolayer
  All sites are equivalent
  Adsorption is independent of coverage
Site conservation
θA + θ* = 1
+
Equilibrium
rateads = ratedes
Irving Langmuir
1932 Nobel Prize

## Slide 20: Using the Langmuir Isotherm
Example: CO adsorption on 10% Ru/Al2O3 @ 100°C
PCO (torr) | 100 | 150 | 200 | 250 | 300 | 400
COads (μmol/gcat) | 1.28 | 1.63 | 1.77 | 1.94 | 2.06 | 2.21
nCO,∞ = 2.89 μmol/gcat
K = 0.0082
10-3 mol Ru
Dispersion
(molCO/molRu) = 0.29%
~1000 atoms

## Slide 21: Brunauer-Emmett-Teller Isotherm (BET)
Relaxes Langmuir restriction to single layer adsorption
  Monolayer adsorption; multilayer condensation
Useful for total surface area measurement
  Adsorption of boiling N2 (78 K)
Solid Surface
ΔHads
ΔHcond
ΔHads/ΔHcond

## Slide 22: Temperature-Programmed Desorption

## Slide 23: Competitive Adsorption

## Slide 24: Rates of Catalytic Reactions
Pseudo-homogeneous reaction rate
  r = moles / volume · time
Mass-based rate
  r′ = moles / masscat · time
  r′ = r / ρcat
Heterogeneous reactions happen at surfaces
Area-based rate
  r′′ = moles / areacat · time
  r′′ = r′ / SA, SA = area / mass
Heterogeneous reactions happen at active sites
Active site-based rate
  Turn-over frequency TOF = moles / site · time
  TOF = r′′ / ρsite
TOF (s−1)
Hetero. cats. ~101
Enzymes ~106

## Slide 25: Surface Reaction Kinetics
Full kinetics
  Site conservation
Langmuir-Hinshelwood kinetics
  Steady-state approximation
  Rate-limiting step approximation
  Pre-equilibrium approximation

## Slide 26: NH3 Oxidation
Friedrich Wilhelm Ostwald
1908 Nobel Prize
Ammonia slip catalyst

## Slide 27: Comparative Bond Forming Pathways
N-N*
N-O*
N-NO*
N-N*
N-O*
N-NO*
Ea,(211)
Ea,(111)
<<
<<
≈
Non-BEP behavior, structure sensitive
Notes: 1. why are NO and N2 barrier heights reversed from product energies on given facet? Agrees with literature?
1. Formation of N2 and NO have much lower barriers. The formation barrier for N2O is similar on both surfaces
2. Right figures are the TS of products formation. The lower barriers of N2 and NO originate from the stabilized transition states on step sites of (211). N2O forms on terrace sites of both surfaces and the reaction barriers are comparable.

## Slide 28: DFT to Reaction Rates and Selectivities
Non-activated adsorption
Reaction Mechanism
Transition State Theory
µkinetic model
Thermodynamic Consistency
Mass + site balances
Coverages
Rates
Surface reactions

## Slide 29: NH3 Oxidation Analysis
Ma and Schneider, ACS Catal. 2019, 9, 2407
Notes: Pt(211) shows much higher rate on Pt(111) at low and intermediate T. The TOF converges at high T.
At low T, multiple reactions control the rate on Pt(211), with barriers lower than 1.6 eV. N2 formation controls the rate on Pt(111), with a much higher barrier, 2.5 eV.
Similarly, between 600~1000K, multiple reactions with low barriers control the rate on Pt(211). NO formation, with a high barrier, controls the rate on Pt(111).
At high T, ammonia activation controls the rates on both surfaces. The reaction has similar barriers and therefore rates on two surfaces.

## Slide 30: Reaction Fluxes and Rate Selectivity
NH3 slip regime
Ostwald regime
Preferred pathways sensitive to facet…
…and to temperature
But products are not!
Notes: At low T, ammonia oxidation is selective to N2. At high T, ammonia oxidation is selective to NO, regardless of the Pt surface and reaction flow pathways.
OH pathway shows more contributions at low T.

## Slide 31: Sabatier Principle
Vojvodic et al. Chem. Phys. Lett. 2014, 598, 108